ITER     –     The Way to Fusion Energy

Material Specification

for the Supply of

austenitic stainless steel seamless tubes

for the ITER divertor

|  | IDM Number: | ITER_D_2A9V93 – v 1.9 | Date 10.05.2011 |
| --- | --- | --- | --- |
|  | Name | Affiliation |  |
| Author | V. Barabash | Materials and Technical Standards Officer |  |
| Reviewers | B. Riccardi S. Suzuki N. Arkhipov F. Escourbiac T. Hirai V. Komarov | EU Divertor Responsible Officer JA Divertor Responsible Officer RF Divertor Responsible Officer IO Divertor Section – PA TRO IO Divertor Section – PA TRO IO Divertor Section – PA TRO |  |
| Approvers | M. Merola | Divertor Section Leader |  |

Table of Content

1	Scope	3

2	Referenced documents	3

2.1	EN and ASTM Standards	3

3	Ordering Information	4

4	Manufacturing Process	4

5	Chemical Requirements and Physico-Chemical Characteristics	4

5.1	Required values	4

5.2	Chemical analysis	4

5.3	Ferrite content and magnetic permeability	4

5.4	Structure and grain size	5

6	Manufacture	5

6.1	Manufacturing programme	5

6.2	Delivery condition	5

7	Mechanical properties	5

7.1	Required values	5

7.2	Technological tests	6

7.3	Retreatment	6

8	Surface Examination – Surface Conditions	6

8.1	Tube surface	6

9	Volumetric Examination	6

10	Removal of Unacceptable Areas	7

11	Dimensions – Tolerances	7

11.1	Tolerances	7

11.2	Dimensional check	7

12	Leak Tightness Test	7

12.1	Hydrostatic test	7

12.2	Eddy current test	7

13	Marking	7

14	Cleanliness-Packaging-Transportation	7

15	Acceptance	8

16	Documentation and Test Report	8

17	Quality Assurance Requirements	8

# Scope

This specification covers austenitic stainless steel seamless tubes grade X2CrNiMo17-12-2, (No. 1.4404) for piping application in the ITER divertor.

This specification is applicable for the first set of the divertor Vertical Targets with CFC/tungsten armour and for the first set of the Dome.

The amount of seamless pipes to be procured shall be specified by the concerned Domestic Agency (DA) and shall include appropriate contingency to face unexpected difficulties, to remake rejected parts and to repair parts with insufficient quality.

The supply covers the following items:

- Manufacture of the total quantity of seamless stainless steel tubes grade X2CrNiMo17-12-2.

- Organisation of quality at works. Elaboration of all procedures required for the manufacturing, inspection (including analyses), packaging, storage and delivery.  Time schedules and documentation.

- To perform all the inspections and tests during and after manufacturing envisaged in this specification.

- Storage, packaging and delivery.

# Referenced documents

The following Codes and Standards shall be referred to in this specification:

## EN and ASTM Standards

EN 10216-5: 2005	Seamless steel tubes for pressure purposes – Technical delivery conditions,

Part 5: Stainless steel tubes

EN 10002-1: 2001	Tensile testing at ambient temperature

EN 10002-5: 1991	Tensile testing at elevated temperature

EN 10246-6: 2000	Non-destructive testing of steel tubes - Part 6: Automatic full peripheral ultrasonic testing of seamless steel tubes for the detection of transverse imperfections.

EN 10246-7: 2006	Non-destructive testing of steel tubes - Part 7: Automatic full peripheral ultrasonic testing of seamless and welded (except submerged arc welded) steel tubes for the detection of longitudinal imperfections.

EN 10246-2:2000	Non-destructive testing of steel tubes - Part 2: Automatic eddy current testing of seamless and welded (except submerged arc-welded) austenitic and ferritic-austenitic steel tubes for verification of hydraulic leak tightness.

EN ISO 643: 2003	Steels – Micrographic determination of the apparent grain size

ASTM A342-04	Standard Test Methods for Permeability of Feebly Magnetic Materials

EN 10204: 2004	Metallic products: Type of inspection documents

Other equivalent national or international standards and codes proposed by DA may be acceptable with prior written IO approval, provided conformity assessment to all criteria is satisfied.

# Ordering Information

It is responsibility of the DA to specify the requirements for the material purchase order.

# Manufacturing Process

The steel shall be made using an electric furnace or by any other technically equivalent process.

Supplier shall propose a detailed manufacturing process, which shall be approved by the IO and DA.

# Chemical Requirements and Physico-Chemical Characteristics

## Required values

The chemical composition determined by ladle and product analyses, shall comply with the requirements given in Table 1.

## Chemical analysis

The chemical analysis shall be performed for each heat of material and .one test shall be performed per lot (test unit).

Table 1. Chemical composition of steel X2CrNiMo17-12-2 (No. 1.4404)

| Element | Alloying elements and impurities content, wt. %. |  |
| --- | --- | --- |
|  | min | max |
| C |  | 0.030 |
| Mn |  | 2.00 |
| Si |  | 1.00 |
| P |  | 0.040 |
| S |  | 0.015 |
| Cr | 16.50 | 18.50 |
| Ni | 10.00 | 13.00* |
| Mo | 2.00 | 2.50 |
| N |  | 0.11 |

* Where for special reasons, e.g. hot workability it is necessary to minimize the delta ferrite content, or with the aim of low permeability, the maximum nickel content may be increased by 1.50 %.

## Ferrite content and magnetic permeability

The ferrite content as evaluated using the Schaeffler diagram, modified by Pryce and Andrews shall be less than 0.5 %, (see note).

The relative magnetic permeability of the finished tubes shall be measured at room temperature after solution annealing. The value measured shall be lower than 1.03 (see note1) (for fields of over 80000A/m (1000Oe) as per Test method 2 or measured with a low μ permeability indicator as per method 3 of ASTM A342. Test shall be performed for 1 sample per lot (test unit).

## Structure and grain size

The structure must be homogeneous.

The microstructural examination to determine grain size is to be in accordance with EN ISO 643. The grain size shall be checked on one tube per lot. The grain size measured shall be equal or greater than No.3.

# Manufacture

## Manufacturing programme

Prior to the commencement of manufacturing operations, the material Supplier shall draw up a manufacturing programme which shall include in chronological order the various manufacturing steps. All intermediate and final heat treatment, finishing and non-destructive examination operations shall be mentioned.

The program shall be agreed with DA and IO.

## Delivery condition

Tubes shall be subjected to solution heat treatment at a temperature between 1020-1120°C prior to delivery. The conditions for solution heat treatment, as well as furnace atmosphere, shall be specified in the manufacturing programme.

# Mechanical properties

## Required values

Tensile strength requirements shall comply with values are given in Table 2.

Table 2. Tensile properties

| Test temperature, °C | Tensile Strength, min, MPa | Yield Strength (0.2%), min, MPa | Longitudinal Elongation, (5d) min, % |
| --- | --- | --- | --- |
| Room | 490 | 190 | 40 |
| 250 | - | 127 | - |

Test for mechanical properties shall be performed per heat and per lot (test unit) as defined in EN 10216-5:2004

Table 3. Number of and content of test

| Name of test | Test temperature (°C) | Number of specimens per type of test |  |
| --- | --- | --- | --- |
|  |  | Per heat | Per lot (test unit) |
| Tension | Room | 1 | 1 |
|  | 250 | 1 | 1 |

- Test method

The tension test shall be performed in compliance with EN 10002-1 at room temperature and in compliance with EN 10002-5 at elevated temperature.

The following values shall be recorded:

  - yield strength at 0.2% offset, in MPa,

  - yield strength at 1% offset, in MPa,

  - ultimate tensile strength, in MPa,

  - percentage elongation after fracture.

## Technological tests

Depending on the tube dimensions one of the test shall be carried out as described in EN 10216-5, chapter 11.3. The tests are flattening or ring expanding or ring tensile or drift expending as described in Chapter 11.3 of EN 10216-5.

## Retreatment

A lot (test unit) rejected on the basis of unsatisfactory results for one or more mechanical tests may be retreated Retreatment conditions shall be described in the test report.

Not more than one retreatment shall be allowed.

# Surface Examination – Surface Conditions

## Tube surface

Internal and external surfaces of tubes shall be sound, i.e. free of any injurious defects as described in EN 10216-5. Straight tubes shall be delivered clean, free of oxidation. Maximum final roughness shall be:

- 6.3 m for the inner and outer surfaces of cold-finished tubes and for the outer surface of hot-finished tubes.

Conditions for visual examinations shall be as in chapter 8.5.1 of EN10216-5.

# Volumetric Examination

Each straight tube shall be subjected to ultrasonic testing for the detection of longitudinal imperfections according to EN 10246-7 and transverse imperfections according to EN 10246-6 to acceptance level U2, sub-category C.

# Removal of Unacceptable Areas

As a general rule, those parts of tubes with unacceptable defects detected by either visual or non-destructive examination shall be discarded.

# Dimensions – Tolerances

## Tolerances

Tube dimension and tolerances shall be in compliance with requirements in the component drawings and shall comply with the requirements of standard EN 10216-5.

## Dimensional check

Each tube shall be inspected.

# Leak Tightness Test

The tubes shall pass a hydrostatic test or an eddy current test for leak-tightness.

## Hydrostatic test

Each tube shall be subjected to hydrostatic testing during finishing operations, in accordance with the requirements specified in EN 10216-5.

## Eddy current test

The test shall be carried out according to EN 10246-2

# Marking

The marking shall include the following information as described in EN 10216-5:

- manufacturer's name or trade mark;

- dimension of the tubes;

- the steel name (or number)

- cast number or a code number;

- test category;

- mark of the inspection representative;

- identification number (e.g. order or item number) which permits the correlation of the product or delivery unit to the related document

# Cleanliness-Packaging-Transportation

Procedures shall be specified in the purchase order.

# Acceptance

Material Test Reports have to be provided to the Purchaser prior to delivery. Material and certification shall be in compliance with this specification. Material cannot be accepted if it does not comply with this specification.

Certification

A certificate, that the material was manufactured, sampled, tested and inspected in accordance with requirements of the material specification and has been found to meet those requirements shall be supplied to the purchaser.

# Documentation and Test Report

The Supplier shall provide the Inspection Certificate type 3.1 in accordance with EN 10204:2004.

The following reports shall be drawn up by the Supplier after each individual test and prior to the delivery of the part:

- heat and product analyses,

- melting process method,

- records of micrographic examination, inclusions and grain size,

- ferrite content and permeability,

- results of mechanical property tests,

- results of technological tests,

- visual examination,

- non-destructive examination,

- dimensional check and roughness.

These reports shall include:

- material designation and marking,

- the heat number and part reference number,

- identification of the Supplier,

- identification of the purchase order number,

- test and retest results together with required values,

- packaging data.

All documents shall be in the English language and all measures shall be given in the metric system SI. Each document shall be provided as an electronic file in PDF format.

# Quality Assurance Requirements

The quality organisation shall comply with the requirements defined in Annex A of the Procurement Arrangement.

Recommendation: the measured values shall be as low as practical.